## Slide 1: Atomic and Ionic Arrangements
OBJECTIVES
relationships between unit cell edge length and atomic radius for FCC and BCC crystal structures
packing factor and density
crystal structure transformation

## Slide 2
Number of atoms per unit cell
  FCC (n = 4)
  SC (n = 1)
  BCC (n = 2)
  HCP (n = 6)
In BCC : Atoms are located and center of the cube
n = 8 corners x (1/8) + 1
In FCC : Atoms are located at the corners and face of the cubes
n = 8 cornes x (1/8) + 6 faces (1/2)
In HCP ;
3 mid plane atoms shared by no other cell : 3 x 1
12 hexagonal corner atoms shared by 6 cells : 12 x (1/6)
2 top/bottom plane atoms shared by 2 cells : 2 x (1/2)

## Slide 3
Atomic Radius vs Lattice Parameters
Directions in the unit cell along which atoms are in continuous contact are close-packed directions.
  SC BCC FCC
ao
ao

## Slide 4
Coordination Number
  The number of atoms touching a particular atom or the number of nearest neighbors is the coordination number.
  Indicates how tightly and efficiently atoms are packed.
Structure | Coordination Number
SC | 6
BCC | 8
FCC | 12
HCP | 12
Maximum

## Slide 5
Atomic Packing Factor (APF)
Theoretical Density
ρmetals> ρceramics > ρpolymers
Both FCC and HCP crystal structures have atomic packing factor of 0.74
Atomic factor of BCC is 0.68
Max. packing factor is = 0.74 (Kepler’s Conjecture)
n = # of atoms
A = atomic weight
VC = UC volume
NA = Avogadro’s number (6.022x1023 atoms/mol)

## Slide 6
Crystal Structure Properties
Donald R. Askeland, Pradeep P. Fulay, Wendelin J. Wright, The Science and Engineering of Materials, Sixth Edition
Crystal Structure | ao | # of Atoms/UC | Coordination Number | Packing Factor
SC | 2r | 1 | 6 | 
BCC | 4r/ | 2 | 8 | 
FCC | 4r/ | 4 | 12 | 
HCP | 2r | 6 | 12 | 
Crystal Structure | ao | # of Atoms/UC | Coordination Number | Packing Factor
SC | 2r | 1 | 6 | 
BCC |  | 2 | 8 | 
FCC |  | 4 | 12 | 
HCP | 2r | 6 | 12 | 

## Slide 7
Allotropic and Polymorphic Transformation
Materials have more than one crystal structure
ALLOTROPY
POLYMORPHISIM
Elements
Compounds
The current crystal structure depends on
1. Temperature
2. Pressure
Cdiamond
Cgraphite

## Slide 8: References
Donald R. Askeland, Pradeep P. Fulay, Wendelin J. Wright, The Science and Engineering of Materials, Sixth Edition
William D. Callister, David G. Rethwisch, Materials Science and Engineering, Eighth Edition, Wiley, 2011.