## Slide 1
Strength of Materials
• Stress and strain
• Elastic behavior/Plastic behavior
• Toughness and ductility
Hardness
Design/Safety Factor

## Slide 2
Hardness
Hardness - Measures the resistance of a material to localized plastic deformation.
It represents resistance to scratching/indentation and a qualitative measure of the strength of the material.
Hardness Tests:
    Simple and inexpensive
    Nondestructive
    It allows to estimate other mechanical properties (tensile strength)
          TS (MPa) = 3.45 x HB (for most steels)
Brinell hardness number

## Slide 3
Hardness:
Macro-hardness: Hardness of materials measured using loads > 2 N.
  Brinell and Rockwell Tests (Different indenters are used)
Micro-hardness: Hardness of materials typically measured using loads less than 2 N
    Knoop (HK)
    Vickers (HV)
Nano-hardness: Hardness of materials measured at 1–10 nm length scale using extremely small (~100 µN) forces.
HB: Brinell hardness number
F: Applied load (kg)
D: Diameter of indenter (mm)
Di: Diameter of the impression (mm)

## Slide 4
Variability of Materials Properties
Measured materials properties (density, modulus of elasticity, electrical conductivity) can scatter by the effects of;
  Test method,
  Variation in specimen fabrication procedure,
  Apparatus calibration,
  Operator bias,
  In-homogenities among the samples.
  The average properties:
  xi : the value of measurement and n: the number of measurements

## Slide 5
Design or Safety Factor
Design approach should be applied to protect against unanticipated failure caused by;
  variability in measured mechanical properties
  imperfections that were introduced through processing
  damage during service
Design stress,
where is calculated stress level and N is design factor (>1)
Safe (working) stress,
where is yield strength.

## Slide 6: References
Donald R. Askeland, Pradeep P. Fulay, Wendelin J. Wright, The Science and Engineering of Materials, Sixth Edition
William D. Callister, David G. Rethwisch, Materials Science and Engineering, Eighth Edition, Wiley, 2011.