## Slide 1: SUTURE MATERIALS AND BASIC SUTURE PATTERNS
Suture materials are classified as absorbable
or nonabsorbable, natural or synthetic, and
monofilament or multifilament, based on composition and structure

## Slide 2: Suture Materials Post Operative Care, Dressing materials Drain Drain Antibiotic Selection
Dr. Murat ÇALIŞKAN

## Slide 3
Materials that lose tensile strength within 60 days of implantation are classified as absorbable; whereas most suture materials will eventually be absorbed.
The truly nonabsorbable sutures are polypropylene and stainless steel.

## Slide 5: ABSORBABLE SUTURE MATERIALS
Surgical gut (catgut) is a natural multifilament suture made from either intestinal submucosa (ovine) or serosa (bovine). It consists of 90% collagen. When cured with chromic salts, surgical gut has increased strength, less inflammatory reaction, and slower absorption. Surgical gut is absorbed by enzymatic digestion and phagocytosis by macrophages. Inflammation,
infection, and catabolic states increase the rate of absorption.

## Slide 6
Polyglactin 910 is a braided multifilament synthetic suture material made of 90% glycolide and 10% L-lactide.
Polyglycolic acid is a multifilament braided synthetic suture material with greater initial strength than surgical gut. Also, in comparison to surgical gut, polyglycolic acid incites less inflammatory reaction.
Polyglycolic acid is absorbed by hydrolysis and has a pattern of loss of strength similar to polyglactin 910

## Slide 7: NONABSORBABLE SUTURE MATERIALS
Silk is the only natural nonabsorbable suture material in common use today. Silk is a braided multifilament suture made from the cocoon of
the silk worm. Silk elicits intense inflammatory reaction and has marked capillarity. It is inexpensive, has excellent handling characteristics,
and has excellent knot security. Coating (wax or silicone) decreases suture capillarity and the tissue’s inflammatory response at the expense
of knot security. Silk must not be applied in infected tissues since it will decrease the number of bacteria necessary to cause a wound infection.

## Slide 8: SURGICAL KNOT TYING